## Slide 1
PART 03
▶
Optimizing Strategies
Strategies for Enhancing Battery Performance and Longevity

## Slide 2
From the Perspective of Electrolyte
Rare Met. 44, 1556–1576 (2025).
Being operated based on solvation reactions
Novel reaction kinetics
Compatible with large sulfur particles
High E/S ratio is necessary
Serve shutting effect
Hard to achieve high loading sulfur cathode
Safety
Pros
Cons
Dissolution-precipitation

## Slide 3
From the Perspective of Electrolyte
Nano Energy, Volume 104, Part B, 2022, 107913
Energy Storage Materials, Volume 38, 2021, 255-261
Low E/S ratio is not suitable because of the sluggish reaction kinetics

## Slide 4
From the Perspective of Electrolyte
Energy Storage Materials, Volume 38, 2021, 255-261
With the decrease of the E/S ratio, the contact angles of the solutions with both the separator and sulfur electrode increase continuously
Indicating a progressively deteriorating wettability
Migration ability of Li+ in the ether electrolyte is also reduced

## Slide 5
What Makes Li-S Batteries distinct from other batteries
From the Perspective of Electrolyte
Boteju, T., et al., 2023
Only responsible for conducting ion
Small amount of electrolyte
Responsible for conducting ion and dissolving polysulfides
Large amount of electrolyte is necessary
Unburden the electrolyte and let it focus on its true purpose

## Slide 6
Weakly Solvating Electrolytes
Nat Energy 3, 783–791 (2018)
To achieve a low E/S ratio cell, it is important to decouple the electrolyte volume and sulfur speciation pathway.
By reducing free solvents, the dissolution of polysulfides is suppressed to realize a quasi-solid-solid reaction.
The sulfur electrochemical reaction is decoupled from the electrolyte volume and effectively inhibits lithium metal side reactions.
3D network/Aggregate
The solubility of

## Slide 7
Weakly Solvating Electrolytes
Nat Energy 3, 783–791 (2018)
Liquid state reaction is gradually converted to be qusai-solid state reaction when solvent is getting less
System with G2:LiTFSI(0.8:1) can run for 100 cycles with the CE of 100%
The issue of corrosion of lithium anode is eased
Reaction kinetics of qusai-solid state reaction is sluggish, leading to limited rate and cycle performance

## Slide 8
Weakly Solvating Electrolytes + Surface-Localized Liquid Phase
Nat. Chem. 17, 614–623 (2025)
Baseline electrolyte configuration: Employing a sparingly-solvating electrolyte to maintain a minimally dissolving effect on lithium polysulfides
Introducing BDTS as a "phase-regulating mediator" to trigger intermolecular chelation with lithium polysulfides
Inducing slight particle dissolution to form a surface-localized liquid phase, thereby accelerating kinetics and conversion

## Slide 9
Weakly Solvating Electrolytes + Surface-Localized Liquid Phase
Nat. Chem. 17, 614–623 (2025)
The Li–S cells achieve excellent kinetics showing 494 mA h -sulfur capacity at a discharge rate of 16C, and stabilized cycling under lean electrolyte (3–5 μl) and high sulfur loading (3–5 mg )